VMZINC ADEKA®® Shingles Roofing & Cladding on vented plywood &

Rainwater Systems – January 24

H74 Zinc strip / sheet coverings / flashings

To be read with preliminaries / general conditions

TYPES OF ZINC WORK

110	ROOFING/CLADDING

•	Roofing system:  VMZINC ADEKA® Shingles, for roof slopes ranging from 15 degrees to 90 degrees.

•	Substrate:  Exterior grade WPB 18mm plywood.  The plywood deck must be even and flush with all joints being less than 2mm in height.  Nails should be driven into the plywood so as to avoid abrasive contact with the underside of the zinc shingles.  Ensure that any treatment which the plywood may have received (fungicides or insecticides) is compatible with the zinc shingles.  A continuous airspace of at least 50mm must be allowed for between the plywood and insulation (which can be protected by the VMZINC membrane).

•	Underlay:  VMZINC membrane to be installed over the plywood.

•	VMZINC:  As clause 520.

-  Standard Finishes:  VMZINC in QUARTZ-ZINC. ANTHRA-ZINC

-  For the following finishes 200m² is required:  PIGMENTO Red, Green, Blue, Brown, Grey, Storm Grey, Charcoal Blue

-  Thickness: 0.7mm

•	Each ADEKA® shingle is fixed using 3 stainless steel screws

- 8.7 ADEKA® units cover 1m² of roofing

•	Ventilated eaves detail:  As clause 340.

•	Ridge/ Hip detail:  Ventilated ridge. As clause 310

•	Verge detail:  Standing seam termination as clause 370.

150	Dormers

•	Dormer zinc:  As clause 520.

-  Finish:  VMZINC PLUS in QUARTZ-ZINC.

-  Thickness:  0.7mm

•	Joints:  ADEKA® shingles or flat lock joints.

210	Gutter lining with expansion joints

•	Gutter: As clause 520.

-  Finish:  VMZINC PLUS in QUARTZ-ZINC.

-  Thickness:  0.7mm or 0.8mm.

•	Joints:  Soldered joints with neoprene at 6m intervals.

Maximum width 600mm.

Minimum fall of 1 in 100 with overflows.

310	Vented ridge/hip detail with minimum 10mm air inlet

•	Ridge:  As clause 520.

-  Finish:  VMZINC in QUARTZ-ZINC.

-  Thickness: 0.7mm or 0.8mm.

•	Joints:  Spacing:  2m.

•	Ridge Cap:

-  Held in place with stainless steel stirrup.

-  ADEKA® ridge strip zinc available in QUARTZ-ZINC (220001141).

340	Vented standing seam eaves with minimum 10mm air inlet

•	Eaves zinc:  As clause 520.

-  Finish: VMZINC PLUS in QUARTZ-ZINC.

-  Thickness: 0.7mm x 235mm width with double fold to receive the key of the ADEKA® shingle.

•	Joints:  Spacing: 2m

•	Eaves Strip:

-  T plate in zinc or galvanized steel.

370	Verge strip

•	Ridge: As clause 520.

-  Finish: VMZINC PLUS in QUARTZ-ZINC.  Contact VMZINC for other finishes.

-  Thickness: 0.7mm

•	Joints:  Spacing:  2m.

•	Top edge:

-  Verge strip receives ADEKA® Shingle.

-  Forming:  Secure top of verge using cleats.

•	Bottom edge:

-  Continuous clip: Fix at 200mm centres.

GENERAL REQUIREMENTS/PREPARATORY WORK

510	WORKMANSHIP GENERALLY

•	Standard: Generally to CP 143-5.

•	Fabrication and fixing:  To provide a secure, free draining and completely weather tight installation.

- Installation company and operatives:  Trained in the application of zinc coverings/ flashings. Submit records of experience on request.  VMZINC at Work installers offer evidence of successfully completed projects, records of VMZINC Training and extended material warranties.

•	Measuring, marking, cutting and forming:  Prior to assembly wherever possible.

•	Metal temperature:  Do not form zinc when the metal temperature is below 7˚C. (10˚C for PIGMENTO).

•	Marking out:  With pencil, chalk or crayon.  Do not use scribers or other sharp instruments without approval.

•	Folding: With mechanical or manual presses to give straight, regular and tight bends, leaving panels free from ripples, kinks, buckling and cracks.  Use hand tools only for folding details that cannot be pressed. The minimum bending radius is thickness x 2 (x 3 for PIGMENTO).

•	Sharp metal edges:  Fold under or remove as work proceeds.

•	Sealants:  Do not use in joints to attain waterproofing.

•	Solder:  Use only where specified.

•	Finished zinc work:  Fully supported, adequately fixed to resist wind uplift and able to accommodate thermal movement without distortion or stress.

•	Protection:  Prevent staining, discolouration and damage by subsequent works. All instructions and recommendations contained in the guidelines for specification and installation of VMZINC standing seam to be applied.  Plastic film must be removed within 2 months of installation and in such a way so as not to trap water between the partially removed film and the zinc.

520	ZINC STRIP/SHEET

•	Zinc-titanium-copper alloy:

-  To BS EN 501 and BS EN 988.

•	Zinc manufactured following ISO 14001 (environmental management), ISO 9001 (quality management) and ISO 18001 safety management.

-  Stamped or labelled with type, finish and thickness.

-  Zinc to be coated on underside with a protective 60 micron lacquer.  ADEKA® Shingles and Ridge cap are manufactured from QUARTZ-ZINC

•	Manufacturer:

-  VMZINC Collier House Mead Lane Hertford Herts SG13 7AX

Tel:  01992 921 300   Email: vmzinc.uk@vmbuildingsolutions.com   Web:  www.vmzinc.co.uk

-  Product reference:

VMZINC in QUARTZ-ZINC and QUARTZ-ZINC PLUS

535	INTEGRITY OF ZINC

•	Requirement:  Design coverings/flashings and methods of attachment to prevent loss of weather tightness and permanent deformation due to wind pressure or suction.

•	Wind loads:  Calculate to BS 6399-2.

555	LAYOUT

•	Setting out of screw positions (280mm c/c – width and 205mm c/c up the roof):  Submit proposals.

610	SUITABILITY OF SUBSTRATES

•	Condition:  Dry and free of dust, debris, grease and other deleterious matter.

620	PREPARATION OF EXISTING TIMBER SUBSTRATES

•	Remedial work: Adjust boards to level and securely fix. Punch in any protruding fasteners and plane or sand to achieve an even surface.

•	Defective boards:  Give notice.

•	Moisture content:  Not more than 22% at time of covering.

FIXING ZINC

710	FIXINGS FOR ADEKA®® Shingles

•	Stainless steel screws

•	Fixing:  Secure each ADEKA® shingle with 3 screws in the holes provided in the shingle. The key at the bottom of the ADEKA®  interlocks into the adjacent shingles.

750	CLIPS FOR FLASHINGS

•	Material:  Zinc of same thickness as that being secured.

•	Dimensions:

-  Width:  Not less than 50mm.

-  Length:  To suit detail.

•	Fixing: Secure each clip to substrate with two fixings not more than 50mm from edge of strip/sheet being fixed.

760	CONTINUOUS CLIPS

Material:  Zinc of same thickness as that being secured.

•	Dimensions:

-  Width:  To suit detail.

-  Length:  Not more than 1.8m.

•	Fixing:  To substrate at 200mm centres.  Welt edge of strip/sheet being fixed to continuous clip and dress down.

810	FORMING DETAILS

•	Folds and welts:  Form without thinning, or splitting the strip/sheet.

•	Thermal movement:  Form details with appropriate allowance for movement, without impairment of security at full expansion or contraction.

825	SOLDERING

•	All zinc must be cleaned back to its natural state.

•	The protective coat on the underside of the upper panel must be removed over a width of 20mm either chemically, using DECALAQ, or mechanically, using a 3 MTM RolocTM  Bristle Disc brush mounted on a small disc sander.

•	The pre-weathering must be removed from the parts to be soldered.  ZINN7 (flux) to be applied to allow spot soldering with solder (40% tin 60% lead)  ZINN7 applied over whole length of joint and then soldered.  Wipe clean

IMPORTANT

All instructions and recommendations contained in the guidelines for specification and installation, published by VMZINC have to be applied.

R10 RAINWATER DRAINAGE SYSTEMS

To be read with Preliminaries/General Conditions.

GENERAL

110	GRAVITY RAINWATER DRAINAGE SYSTEM VMZINC Rainwater system Half Round and Boxed

•	Gutters, downpipes and all accessories (excluding brackets) in QUARTZ-ZINC or ANTHRA-ZINC.

•	Below ground drainage:  Submit proposals.

•	Disposal: To soak away as section R12.

SYSTEM PERFORMANCE

210	DESIGN

•	Design:  Complete the design of the rainwater drainage system.

•	Standard:  To BS EN 12056-3 : 2000.

•	Proposals:  Submit drawings, technical information, calculations and manufacturers' literature.

221	COLLECTION AND DISTRIBUTION OF RAINWATER

•	General:  Complete and without leakage or noise nuisance.

230	DESIGN PARAMETERS - GENERAL

•	Roof and gutter construction and finish:  QUARTZ-ZINC or ANTHRA-ZINC.

•	Design rate of rainfall:  As BS EN 12056-3, National Annex NB.2. Category: 4.

•	Available capacity of existing below ground drainage (maximum):  To be determined by Architect/Engineer.

355	ZINC GUTTERS

•	Manufacturer:

-  VMZINC Collier House Mead Lane Hertford Herts SG13 7AX

Tel:  01992 921 300   Email: vmzinc.uk@vmbuildingsolutions.com   Web:  www.vmzinc.co.uk

-  Product reference:  VMZINC rainwater system Half Round and Boxed

•	Profile: Half round gutter, ref: 250 or

Half round gutter, ref: 333 or

Box gutter, ref: 333 or

Profiled gutter, ref: 333.

•	Thickness: 0.7 mm.

•	Brackets:  Galvanized steel and zinc, fascia type.

-  Fixings: Stainless steel screws.  	Size: 30 x 4 mm.

•	Accessories: Half round gutter, ref: 250 and 333:

Stop ends

Exterior corner

Interior corner

Hopper

Downpipe bend

Universal outlet

Rainwater diverter

360	SEALANT/SOLDER FOR VMZINC RAINWATER SYSTEMS

•	Type VMZINC Half Round Gutter – VMZINC adhesive

•	Type VMZINC Boxed Gutter– Tin/lead solder

EXECUTION

600	PREPARATION

•	Work to be completed before commencing work specified in this section:

-  Below ground drainage.  Alternatively, make temporary arrangements for dispersal of rainwater without damage or disfigurement of the building fabric and surroundings.

605	INSTALLATION GENERALLY

•	Electrolytic corrosion:  Avoid contact between dissimilar metals where corrosion may occur.

•	Allowance for thermal and building movement:  Provide and maintain clearance as fixing and jointing proceeds.

•	Protection:

-  Fit purpose made temporary caps to prevent ingress of debris.   Fit access covers, cleaning eyes and

blanking plates as the work proceeds.

610	FIXING AND JOINTING GUTTERS

•	Joints:  Silicone Adhesive or solder as per clause 360.

•	Brackets: Securely fixed.

-  Fixings: To be determined by Architect / Engineer].  Fixing centres:  400mm.

-  Additional brackets:  Where necessary to maintain support and stability, provide at joints in gutters and

near angles and outlets.

•	Roofing underlay:  Dressed into gutter.

615	SETTING OUT EAVES GUTTERS - TO FALLS

•	Setting out:  To true line and even gradient to prevent ponding or back fall.  Position high points of gutters as close as practical to the roof and low points not more than 50mm below the roof.  Minimum fall to be 1 in 200.

•	Outlets:  Align with connections to below ground drainage.

630	INSTALLING RAIN WATER OUTLETS

•	Fixing: Secure. Fix before connecting pipe work.

•	Junctions between outlets and pipe work:  Accommodate movement in structure and pipe work.

635	FIXING PIPE WORK

•	Pipe work:  Fix securely, plumb and/or true to line.

•	Branches and low gradient sections:  Fix with uniform and adequate falls to drain efficiently.

•	Externally socketed pipes and fittings:  Fix with sockets facing upstream.

•	Additional supports:  Provide as necessary to support junctions and changes in direction.

•	Vertical pipes:

-  Provide a load bearing support at least at every storey/level.

-  Tighten fixings as work proceeds so that every storey is self-supporting.

-  Wedge joints in unsealed metal pipes to prevent rattling.

•	Wall and floor penetrations:  Isolate pipe work from structure.

-  Pipe sleeves:  As section P31.

-  Masking plates:  Fix at penetrations if visible in the finished work.

•	Expansion joint pipe sockets:  Fix rigidly to buildings.  Elsewhere, provide brackets and fixings that allow pipes to slide.

640	FIXING VERTICAL PIPE WORK

•	Bracket fixings:  To be determined by Architect/Engineer].

•	Distance between bracket fixing centres (maximum):  1000mm.

650	JOINTING PIPE WORK AND GUTTERS

•	General: Joint with materials and fittings that will make effective and durable connections.

•	Jointing differing pipe work and gutter systems:  Use adaptors intended for the purpose.

•	Cut ends of pipes and gutters:  Clean and square.  Remove burrs and swarf.  Chamfer pipe ends before inserting into ring seal sockets.

•	Jointing or mating surfaces:  Clean and, where necessary, lubricate immediately before assembly.

•	Junctions:  Form with fittings intended for the purpose.

•	Jointing material:  Strike off flush.  Do not allow it to project into bore of pipes and fittings.

•	Surplus flux, solvent jointing materials and cement:  Remove.

700	ACCESS FOR TESTING AND MAINTENANCE

•	General: Install pipe work and gutters with adequate clearance to permit testing, cleaning and maintenance.

COMPLETION

900	TESTING GENERALLY

•	Dates for testing: Give notice.

-  Period of notice (minimum):  To be determined by Architect/Engineer.

•	Preparation:

-  Pipe work: Complete, securely fixed, free from defects, obstruction and debris before testing.

•	Testing:

-  Supply clean water, assistance and apparatus.

-  Do not use smoke to trace leaks.

•	Records: Submit a record of tests.

905	INTERNAL PIPE WORK TEST - ENGLAND, WALES, IRELAND AND NORTHERN IRELAND

•	Preparation: Temporarily seal open ends of pipe work with plugs.

•	Test apparatus:  Connect a 'U' tube water gauge and air pump to pipe work via a plug.

•	Testing: Pump air into pipe work until gauge registers 38 mm.

•	Required performance:

-  Allow a period for temperature stabilization, after which the pressure of 38 mm is to be maintained

Without loss for at least 3 minutes.

906	INTERNAL PIPE WORK TEST - SCOTLAND

•	Standard:  To BS EN 12056-2, National annex NG.

910	GUTTER TEST

•	Preparation:  Temporarily block all outlets.

•	Testing:  Fill gutters to overflow level and after 5 minutes closely inspect for leakage.

915	MAINTENANCE INSTRUCTIONS

•	General:  At completion, submit printed instructions recommending procedures for maintenance of the rainwater installation, including full details of recommended inspection, cleaning and repair procedures.

920	IMMEDIATELY BEFORE HANDOVER

•	Construction rubbish, debris, swarf, temporary caps and fine dust which may enter the rainwater system: Remove.  Do not sweep or flush into the rainwater system.

•	Access covers, Rodding eyes, outlet gratings and the like:  Secure complete with fixings.

IMPORTANT

All instructions and recommendations contained in the guidelines for specification and installation, published by VMZINC have to be applied.